## Slide 1: 2016-23rd IFHTSE Conference
Hot Hydroforging of Lightweight Bimaterial Gears and Hollow Products
Bulent Chavdar1, Robert Goldstein2, Lynn Ferguson3
1Eaton, Southfield, MI, USA
2Fluxtrol Inc., Auburn Hills, MI, USA
3DANTE Solutions Inc., Cleveland, OH, USA
April 20, 2016

## Slide 2: What is Hot hydroforging?
Definition: Hot forging of lightweight products from a hybrid billet of a metal shell and a low melting core.
Concept: Hot hydroforging is done at temperatures where the core material is in viscous state and builds up uniform pressure thereby enabling a uniform deformation of the metal shell.
Goal: Lightweight net shape forging with complex topologies
Viscous core
Core is squeezed
out of center.

## Slide 3: Hybrid lightweight gear
The outer structure is steel, the inner structure is a low melting lightweight material.

## Slide 4: Objectives
Forging light weight hybrid gears with net teeth and near net center.
The hybrid gear has all steel outer structure.
Investment forging is enabled (molten core can be emptied).
Press loads are reduced and larger gears can be forged.
30% to 50% weight reduction per gear is targeted.
60% to 70% reduction in machining scrap rate due to near net teeth.

## Slide 5: Steels and low melting point materials

## Slide 6: FEA modeling of stand-alone hybrid gear Loads, BCs and Contacts
Ft (N) | Fr (N) | Resultant (N)
-22638 | -8500 | 24181
Gear Loads
Cylindrical support
Bonded contact between Inner Al and Outer Steel.

## Slide 7: Stress plots
Max von-Mises stress at fillet = 172.4 MPa
Max Principal stress at fillet = 164.5 MPa

## Slide 8: Wall thickness optimization-Steel/Al gear Trade off between weight reduction and stress increase
Steel wall Thickness (mm) | Weight reduction (%) | von-Mises stress (MPa) | Stress Increase (%) | Weight reduc. penalty
All steel |  | 128 |  | 
1.5 | 40 | 172 | 34 | 0.85
2.5 | 35 | 158 | 23 | 0.66
3.5 | 30 | 152 | 19 | 0.63
Optimum steel
wall thickness

## Slide 9: Wall thickness optimization-Hollow gear Trade off between weight reduction and stress increase
Steel wall Thickness (mm) | Weight reduction (%) | von-Mises stress (MPa) | Stress Increase (%) | Weight reduc. penalty
All steel |  | 128 |  | 
1.5 | 61 | 433 | 238 | 3.9
2.5 | 53 | 280 | 119 | 2.2
3.5 | 46 | 211 | 65 | 1.4
4.5 | 40 | 162 | 27 | 0.7
5.5 | 35 | 150 | 17 | 0.5
1.5 mm wall
2.5 mm wall
Hollow gear

## Slide 10: Hybrid billet design for hot hydroforging
Cap
Tube
Al bar
Steel tube
seamless, and w/ seam
0.25” and 0.5” wall
Weld bead
Electron beam welding
Interference fit
0.003”, and 0.005”
Factors Levels
Wall thickness 0.25” (6.25 mm) 0.5” (12.5 mm)
Steel tube type seamless with seam
Interference fit 0.003”(0.075mm) 0.005” (0.125 mm)
Forging technique Hot (solid state) Hot hydroforging

## Slide 11: Die design and simulations
Weld bead
Electron beam welding
The pockets in the top and the bottom dies keep the weld zone of end caps under compression during busting forging.
Before forging
After forging
Forged part
Closed and split die

## Slide 12: Solid state hot forging simulations
Solid state forging simulations predicted folds, shrinkage gap and non-uniform steel wall thickness.

## Slide 13: Forging trials
Erie 4000 ton mechanical press
Bi-Metal billets before forging
10 kHz Induction heater
Heating
Transferred to the die
Right after forging
A few seconds after forging
Forged parts
Forged parts

## Slide 14: Comparison of hot forging and hot hydroforging experiments
Solid state hot forging
Steel @1100C
Al core @400C
Hot hydroforging
Steel @1100C
Al core @1100C
Fractured wall
Incomplete fill
Fold
Non-uniform wall
Gap due to CTE mismatch
No fracture or crack
Cracks
Uniform wall
Void due to CTE mismatch
Hot hydroforging is promising
if CTE mismatch is eliminated
Not successful
Successful

## Slide 15: Weld zone healing in hot hydroforging
Before forging
Dendritic structure
After busting hot hydroforging
Normalized structure
Dendritic structure of weld zone disappeared after hot hydroforging

## Slide 16: “Investment Forging”
Investment forging is a term coined at Eaton.
It describes a process where the molten core is evacuated from the forged part after a hot hydroforging process leaving behind a hollow part.
Investment forging provides the ultimate weight reduction up to 50% for a gear.
Investment forging can also be applied to many other forged parts. For example forged hollow engine exhaust valves can be created by investment forging.
Steel
eb weld
Core
emptied
Low melting
core

## Slide 17: Eliminating CTE mismatch with glass
Glass is identified as the core material of choice with matching CTE to that of steel, 10-12 (10-6 m/mK).
The other advantages of glass:
  Low cost
  Low density
  Good bonding to steel
  Lower elastic modulus than steel
  Working temperature can be optimized
  May enable and temper a through-hardened steel wall

## Slide 18: Induction heating / air cooling simulations Displacement and gap formation in solid state
Steel/Glass
Steel/Aluminum
No gap predicted
Significant gap predicted
Glass is a promising lightweight core material.

## Slide 19
N165 is on steel bore, and N4442 is on outer surface of core.
Steel/Glass
Steel/Aluminum
No gap predicted
Significant gap predicted
*
*
*
Induction heating / air cooling simulations
Histories of displacements and gap formation in solid state
Air cooling
Induction
heating
Air cooling
Induction
heating

## Slide 20: Furnace heating / air cooling simulations of steel/glass History of displacements and gap formation (no phase change)
No gap predicted
Assumed no bonding between steel and glass.
In reality steel and glass will bond. There will be no gap.
Steel/glass billets can be heated in furnace without fracture.
Steel/aluminum cannot be heated in furnace without fracture.
Furnace heating
Air cooling
No gap
at mid height
32 mm gap
in upper and
lower halves

## Slide 21: Stress histories and final stress states in steel/glass after furnace heating and air cooling
Axial stress histories on various locations on steel cylinder.
* The highest axial stress occurs at the inner corner of steel end cap and the steel cylinder
Final stress states
*

## Slide 22: Conclusions
Feasibility of hot hydroforging and investment forging for lightweighting, net shape forging and waste reduction are demonstrated.
Steel/aluminum hybrid billets were prepared. Then, the billets were hot hydroforged in closed dies.
A uniform steel wall thickness was observed all around the hot hydroforged part upon cross sectioning.
Weld seams are healed (normalized) upon hot hydroforging.
Steel/glass is a more promising hybrid than steel/aluminum for hot hydroforging due to the CTE match.

## Slide 24: Back up slides

## Slide 25: High frequency induction power 10 kHz, 500 kW
Induction heater controller
Coil for high frequency induction heating

## Slide 26: Induction heating simulations for solid state hot forging Temperature vs. time in the radial direction
Ramp
Hold
Transfer
Al Core
Steel Case
Chart: Temperature (C)
| 0.0 | 0.00089 | 0.00178 | 0.00266999999999999 | 0.00356 | 0.00445 | 0.00533999999999999 | 0.00622999999999999 | 0.00712 | 0.00801 | 0.0089 | 0.00979 | 0.0106799999999999 | 0.0115699999999999 | 0.0124599999999999 | 0.0133499999999999 | 0.01424 | 0.01513 | 0.01602 | 0.0169099999999999 | 0.0178 | 0.01869 | 0.01958 | 0.02047 | 0.0213599999999999 | 0.02225 | 0.0231399999999999 | 0.02403 | 0.0249199999999999 | 0.02581 | 0.0266999999999999 | 0.02759 | 0.02848 | 0.0293699999999999 | 0.03026 | 0.0311499999999999 | 0.03204 | 0.03293 | 0.0338199999999999 | 0.03471 | 0.0356 | 0.0364899999999999 | 0.03738 | 0.03827 | 0.03916 | 0.0400499999999999 | 0.04094 | 0.04183 | 0.0427199999999999 | 0.0436099999999999
T = 2 | 20.4089 | 20.4098 | 20.4123 | 20.4167 | 20.4227 | 20.4306 | 20.4403 | 20.4519 | 20.4654 | 20.481 | 20.4987 | 20.5186 | 20.5409 | 20.5656 | 20.5929 | 20.623 | 20.656 | 20.6921 | 20.7315 | 20.7744 | 20.821 | 20.8717 | 20.9267 | 20.9862 | 21.0506 | 21.1203 | 21.1957 | 21.277 | 21.3648 | 21.4595 | 21.5616 | 21.6716 | 21.7901 | 21.9177 | 22.055 | 22.2027 | 101.265 | 105.3798 | 113.8257 | 126.8499 | 144.8848 | 168.5662 | 198.761 | 236.7235 | 284.1533 | 343.3074 | 417.685 | 511.5875 | 629.8494 | 761.6482
t = 4 | 24.022 | 24.0266 | 24.0405 | 24.0636 | 24.0961 | 24.138 | 24.1894 | 24.2505 | 24.3215 | 24.4024 | 24.4935 | 24.5951 | 24.7074 | 24.8307 | 24.9652 | 25.1114 | 25.2696 | 25.4402 | 25.6235 | 25.8201 | 26.0304 | 26.255 | 26.4942 | 26.7488 | 27.0193 | 27.3063 | 27.6105 | 27.9325 | 28.2731 | 28.633 | 29.013 | 29.4139 | 29.8365 | 30.2817 | 30.7503 | 31.2434 | 271.1904 | 279.1126 | 293.8125 | 315.5669 | 344.9444 | 382.8256 | 430.4875 | 489.5889 | 562.7793 | 653.7636 | 760.3553 | 873.8969 | 962.3376 | 1016.1906
t = 6 | 33.3866 | 33.3961 | 33.4245 | 33.4719 | 33.5384 | 33.6241 | 33.729 | 33.8533 | 33.9972 | 34.1607 | 34.3443 | 34.548 | 34.7722 | 35.0171 | 35.283 | 35.5703 | 35.8792 | 36.2103 | 36.5639 | 36.9404 | 37.3402 | 37.764 | 38.212 | 38.6848 | 39.1831 | 39.7073 | 40.258 | 40.8359 | 41.4415 | 42.0754 | 42.7384 | 43.4311 | 44.1542 | 44.9084 | 45.6945 | 46.513 | 429.7299 | 439.572 | 455.7975 | 478.4861 | 507.7538 | 543.7668 | 586.7584 | 637.4129 | 697.9146 | 768.867 | 841.3412 | 902.033 | 946.7861 | 973.0839
t = 8 | 48.8993 | 48.9126 | 48.9523 | 49.0184 | 49.1112 | 49.2305 | 49.3765 | 49.5493 | 49.7489 | 49.9756 | 50.2293 | 50.5105 | 50.819 | 51.1553 | 51.5194 | 51.9117 | 52.3323 | 52.7816 | 53.2597 | 53.767 | 54.3037 | 54.8702 | 55.4669 | 56.094 | 56.7519 | 57.441 | 58.1617 | 58.9144 | 59.6994 | 60.5173 | 61.3683 | 62.253 | 63.1718 | 64.1251 | 65.1135 | 66.1373 | 536.987 | 547.2993 | 562.5276 | 582.7366 | 608.0212 | 638.9342 | 676.3223 | 721.3302 | 775.0942 | 831.326 | 881.2126 | 922.5324 | 953.1807 | 971.4654
t = 10 | 68.9385 | 68.954 | 69.0007 | 69.0784 | 69.1873 | 69.3273 | 69.4986 | 69.7011 | 69.9351 | 70.2004 | 70.4972 | 70.8257 | 71.1859 | 71.5779 | 72.0019 | 72.4581 | 72.9465 | 73.4674 | 74.0209 | 74.6072 | 75.2265 | 75.879 | 76.5649 | 77.2845 | 78.0379 | 78.8254 | 79.6472 | 80.5037 | 81.3951 | 82.3216 | 83.2835 | 84.2811 | 85.3148 | 86.3848 | 87.4913 | 88.6348 | 610.5207 | 621.2728 | 636.162 | 655.4974 | 679.7243 | 709.5061 | 746.6116 | 791.4645 | 837.9532 | 881.1286 | 919.7672 | 952.2096 | 977.0438 | 992.2247
t = 12 | 92.0435 | 92.0604 | 92.1111 | 92.1956 | 92.3139 | 92.466 | 92.6521 | 92.872 | 93.1259 | 93.4138 | 93.7358 | 94.0919 | 94.4822 | 94.9068 | 95.3658 | 95.8593 | 96.3873 | 96.95 | 97.5475 | 98.18 | 98.8475 | 99.5502 | 100.2882 | 101.0617 | 101.8709 | 102.7158 | 103.5968 | 104.514 | 105.4675 | 106.4576 | 107.4845 | 108.5483 | 109.6493 | 110.7877 | 111.9638 | 113.1777 | 665.4323 | 677.0873 | 692.6987 | 712.7098 | 738.5746 | 772.0965 | 811.5054 | 851.4817 | 890.3388 | 927.1796 | 960.6744 | 989.7177 | 1012.6085 | 1026.8041
t = 14 | 117.1345 | 117.1522 | 117.2053 | 117.2939 | 117.4178 | 117.5773 | 117.7722 | 118.0027 | 118.2687 | 118.5702 | 118.9074 | 119.2802 | 119.6888 | 120.1331 | 120.6133 | 121.1294 | 121.6814 | 122.2695 | 122.8938 | 123.5543 | 124.2512 | 124.9845 | 125.7543 | 126.5608 | 127.4041 | 128.2844 | 129.2016 | 130.1561 | 131.1479 | 132.1772 | 133.2441 | 134.3489 | 135.4916 | 136.6725 | 137.8917 | 139.1494 | 710.3877 | 723.2852 | 741.4315 | 766.4524 | 798.2433 | 833.2279 | 869.1527 | 905.511 | 941.3877 | 975.8818 | 1008.0724 | 1036.4776 | 1059.0552 | 1073.0352
t = 16 | 143.4693 | 143.4875 | 143.5423 | 143.6335 | 143.7612 | 143.9254 | 144.1262 | 144.3636 | 144.6375 | 144.9481 | 145.2953 | 145.6792 | 146.0998 | 146.5573 | 147.0517 | 147.5829 | 148.1512 | 148.7565 | 149.399 | 150.0788 | 150.7959 | 151.5504 | 152.3425 | 153.1723 | 154.0398 | 154.9454 | 155.8889 | 156.8707 | 157.8909 | 158.9497 | 160.0472 | 161.1836 | 162.3591 | 163.5739 | 164.8282 | 166.1223 | 754.4209 | 770.8502 | 794.4556 | 822.4185 | 852.6671 | 884.6588 | 917.9589 | 951.6491 | 985.0767 | 1017.4281 | 1047.4771 | 1073.7596 | 1094.333 | 1106.632
t = 18 | 170.9831 | 171.0025 | 171.0608 | 171.158 | 171.294 | 171.469 | 171.683 | 171.936 | 172.2282 | 172.5595 | 172.9302 | 173.3402 | 173.7897 | 174.2788 | 174.8077 | 175.3765 | 175.9854 | 176.6345 | 177.3241 | 178.0543 | 178.8254 | 179.6375 | 180.491 | 181.386 | 182.3229 | 183.3018 | 184.3232 | 185.3872 | 186.4943 | 187.6447 | 188.8388 | 190.0769 | 191.3594 | 192.6863 | 194.0569 | 195.4656 | 823.156 | 839.1906 | 859.4175 | 883.2946 | 910.3007 | 939.5227 | 970.1807 | 1001.5281 | 1032.6348 | 1062.4285 | 1089.7581 | 1113.2324 | 1131.0765 | 1141.1427
t = 20 | 199.9086 | 199.9293 | 199.9914 | 200.095 | 200.2401 | 200.4266 | 200.6547 | 200.9244 | 201.2358 | 201.5888 | 201.9836 | 202.4204 | 202.899 | 203.4198 | 203.9827 | 204.588 | 205.2357 | 205.926 | 206.659 | 207.4349 | 208.2539 | 209.1162 | 210.0218 | 210.9712 | 211.9643 | 213.0016 | 214.0831 | 215.2092 | 216.38 | 217.5959 | 218.8571 | 220.1639 | 221.5164 | 222.9147 | 224.3578 | 225.8395 | 884.2865 | 900.2795 | 919.441 | 941.3991 | 965.7615 | 992.0551 | 1019.6911 | 1047.8855 | 1075.8364 | 1102.6384 | 1127.1739 | 1148.1558 | 1164.0004 | 1172.6623
t = 22 | 229.6717 | 229.6933 | 229.758 | 229.866 | 230.0171 | 230.2115 | 230.4491 | 230.73 | 231.0542 | 231.4218 | 231.8329 | 232.2874 | 232.7855 | 233.3273 | 233.9127 | 234.542 | 235.2152 | 235.9324 | 236.6937 | 237.4992 | 238.3491 | 239.2434 | 240.1824 | 241.1661 | 242.1946 | 243.2682 | 244.3869 | 245.5509 | 246.7604 | 248.0155 | 249.3163 | 250.6631 | 252.0558 | 253.4944 | 254.9779 | 256.5014 | 936.1206 | 952.0301 | 970.5685 | 991.4812 | 1014.4152 | 1038.8492 | 1064.2199 | 1089.8933 | 1115.1298 | 1139.0254 | 1160.6158 | 1178.7552 | 1192.0114 | 1198.6111
t = 24 | 259.6336 | 259.6556 | 259.7216 | 259.8316 | 259.9856 | 260.1837 | 260.4258 | 260.7119 | 261.0422 | 261.4166 | 261.8352 | 262.298 | 262.8051 | 263.3566 | 263.9524 | 264.5927 | 265.2775 | 266.0069 | 266.781 | 267.6 | 268.4637 | 269.3725 | 270.3264 | 271.3254 | 272.3698 | 273.4596 | 274.595 | 275.7762 | 277.0032 | 278.2762 | 279.5954 | 280.961 | 282.373 | 283.8314 | 285.3354 | 286.8808 | 977.5576 | 992.976 | 1010.3194 | 1029.2888 | 1049.5259 | 1070.6106 | 1092.0646 | 1113.3355 | 1133.7761 | 1152.7273 | 1169.4462 | 1183.0676 | 1192.5291 | 1196.515
Al Core
Steel Case
Both steel and aluminum are in solid state
Due to differential heating rate steel shell pulled away from the core

## Slide 27: Billet induction heating simulations for hot hydroforging, on-off control strategy
Iso-temperature lines showing the temperature distribution in the radial direction from the center axis to the outer diameter of the billet at mid height of the billet as function of the heating time. The heating simulation shows the effect of on/off control strategy
Heating simulation shows that aluminum core reaches 1000C in 6 on/off cycles in 60 seconds

## Slide 28: FEA of subassembly with hybrid gears
Steel on the outside
Aluminum in the core
Gear B
Gear D

## Slide 29: Force reactions at bearing supports and torsional spring at end face
Bearing Front
Torsional spring at end face
Bearing Rear
Global deformation of assembly
reduces stress concentration

## Slide 30: Subassembly deformation and stress All steel gear and hybrid forged gear
 | Hybrid-Bi-Metal forging |  |  | All Steel |  | 
 | Gear B | Gear D | Countershaft | Gear B | Gear D | Countershaft
Total (mm) | 0.48 | 0.425 | 0.297 | 0.46 | 0.421 | 0.294
Angular (0) | 0.31 | 0.31 | 0.31 | 0.3 | 0.3 | 0.3
Radial (mm) | -0.063 | -0.127 | -0.127 | -0.06 | -0.122 | -0.123
Axial (mm) | 0.081 | -0.0442 | 0.032 | 0.077 | -0.043 | 0.031
 | Hybrid-Bi-Metal forging |  | All Steel | 
 | Gear B | Gear D | Gear B | Gear D
Von-Mises | 825 | 876 | 761 | 745
Max principal | 730 | 729 | 696 | 674
Min principal | -934 | -978 | -859 | -831
No stress or deflection is increased more than 8% for the bimetal gear compared to the all-steel gear
Deformations
Stresses (MPa)

## Slide 31: Die stress analysis
Chart: Normal Pressure on the die
a
b
c
d
e
e
d
c
b
a
Ram displacement (mm/406mm) | Forge load (ton) | Fill radius, d (mm) | Stress at the die fillet, d (MPa)
405.90 | 973 | 1.50 | 2120
405.87 | 758 | 2.30 | 1750
405.68 | 552 | 4.25 | 1320
Forging
temperature: 1100C